## Slide 1: General overview

## Slide 2
Waste
Eluent
Eluent pump
Heat and stir plate
Polymer pump
Dialysis module
Purge
solvent
NMR
Overpressure release
Deuterated solvent
MeOH
Purge
solvent
Stock solutions
10 mL syringe pump
Argon supply
UV/VIS
Solenoid valve
Precipi-tation vessel
Gas manifold
Linear actu-ator
For all connections, 0.75 mm i.d. tubing was used (o.d. = 1/16 “)
General overview
Gas in: always port H
Purge solvent in: always port G
To reaction vial: always port A
To waste: always port E

## Slide 3: General overview with info about tubing or COM ports, etc

## Slide 4
Waste
Eluent
Eluent pump
Heat and stir plate
Polymer pump
Dialysis module
Purge
solvent
NMR
Overpressure release
Deuterated solvent
MeOH
Purge
solvent
Stock solutions
10 mL syringe pump
Argon supply
UV/VIS
Solenoid valve
Precipi-tation vessel
Gas manifold
Linear actu-ator
For all connections, 0.75 mm i.d. tubing was used (o.d. = 1/16 “)
Volume of relevant tubing
Gas in: always port H
Purge solvent in: always port G
To reaction vial: always port A
To waste: always port E
Cuvette volume = 140 µL
Ca. 88 µL
Ca. 199 µL
Ca. 199 µL
Ca. 248 µL
Ca. 309 µL
Ca. 177 µL
Ca. 110 µL
Ca. 353 µL
Ca. 177 µL
Ca. 2.4 mL (icluding NMR glass flow cell)
Ca. 252 µL
Ca. 132 µL
Ca. 243 µL
Ca. 243 µL
Ca. 292µL
Ca. 250µL
Ca. 167µL
Ca. 167µL
Ca. 125µL
Ca. 138µL
Ca. 179 µL
Ca. 3.2 mL
Ca. 110 µL
Ca. 234 µL
Ca. 420 µL
Ca. 177 µL
Ca. 3.2 mL
Ca. 123 µL
Ca. 256 µL

## Slide 5
Waste
Eluent
Eluent pump
Heat and stir plate
Polymer pump
Dialysis module
Purge
solvent
NMR
Overpressure release
Deuterated solvent
MeOH
Purge
solvent
Stock solutions
10 mL syringe pump
Argon supply
UV/VIS
Solenoid valve
Precipi-tation vessel
Gas manifold
Linear actu-ator
For all connections, 0.75 mm i.d. tubing was used (o.d. = 1/16 “)
Length of relevant tubing
Gas in: always port H
Purge solvent in: always port G
To reaction vial: always port A
To waste: always port E
Ca. 57 cm
Ca. 73 cm + NMR glass flow cell
Ca. 20 cm
Ca. 45 cm
Ca. 45 cm
Ca. 56 cm
Ca. 70 cm
Ca. 40 cm
Ca. 25 cm
Ca. 80 cm
Ca. 40 cm
Ca. 55 cm
Ca. 55 cm
Ca. 30 cm
Ca. 25 cm
Ca. 70 cm
Ca. 60 cm
Ca. 40 cm
Ca.40 cm
Ca. 30 cm
Ca. 43 cm
Ca. 33 cm
Ca. 53 cm
Ca. 10 cm
Ca. 40 cm
Ca. 75 cm
Ca. 28 cm
Ca.10 cm
Ca. 58 cm

## Slide 6
Waste
Eluent
Eluent pump
Heat and stir plate
Polymer pump
Dialysis module
Purge
solvent
NMR
Overpressure release
Deuterated solvent
MeOH
Purge
solvent
Stock solutions
10 mL syringe pump
Argon supply
UV/VIS
Solenoid valve
Precipi-tation vessel
Gas manifold
Linear actu-ator
For all connections, 0.75 mm i.d. tubing was used (o.d. = 1/16 “)
Overview of COM ports, etc.
Gas in: always port H
Purge solvent in: always port G
To reaction vial: always port A
To waste: always port E
COM12
USB
?
COM12
COM7 Adress: 1
COM12
COM14
COM16
Adress: 2
COM15
Adress: 1
COM7
Adress: 3
COM7
Adress: 2
COM7
Adress: 4

## Slide 7
Waste
Eluent
Eluent pump
Heat and stir plate
Polymer pump
Dialysis module
Purge
solvent
NMR
Overpressure release
Deuterated solvent
MeOH
Purge
solvent
Stock solutions
10 mL syringe pump
Argon supply
UV/VIS
Solenoid valve
Precipi-tation vessel
Gas manifold
Linear actu-ator
For all connections, 0.75 mm i.d. tubing was used (o.d. = 1/16 “)
In Medusa Graph (for most liquid transfers) - Denomination
Gas in: always port H
Purge solvent in: always port G
To reaction vial: always port A
To waste: always port E
COM12
USB
?
COM12
COM7 Adress: 1
COM12
COM14
COM16
Adress: 2
COM15
Adress: 1
COM7
Adress: 3
COM7
Adress: 2
COM7
Adress: 4
“NMR”
“Deuterated_Solvent”
“UV_VIS”
“Gas_Reservoir_Vessel”
“Precipitation_Pump”
“Precipitation_Vessel_Dispense”
“Methanol_Vessel”
“Waste_Vessel”
“Solvent_Monomer_Modification_Pump”
“Initiator_CTA_Pump”
“Purge_Solvent_Vessel_1”
“CTA_Vessel”
“Initiator_Vessel”
“Solvent_Vessel”
“Monomer_Vessel”
“Modification_Vessel”
“Hotplate”
“Reaction_Vial”
“Analytical_Pump”
“Purge_Solvent_Vessel_2”
“Precipitation_Vessel_Solenoid”
“Linear_Actuator”
“Gas_Valve”
“Precipitation_Valve”
“Polymer_Peri_Pump”
“Solvent_Peri_Pump”

## Slide 8: Overview of individual modules

## Slide 9
Argon supply
Waste
Heat and stir plate
Purge
solvent
NMR
Overpressure release
Deuterated solvent
Purge
solvent
Stock solutions
10 mL syringe pump
Gas manifold
Linear actu-ator
Module 1 – Polymerization module
Gas in: always port H
Purge solvent in: always port G
To reaction vial: always port A
To waste: always port E
0. Manual preparation of stock solutions (CTA, AIBN, Solvent, Monomer); Preheating of heat and stir plate.
Formulation of polymerization solution.
2. Deoxygenation for 20 min with argon sparging.
3. Insertion of polymerization vial to heat block.
4. Online monitoring of conversion.
5. After 80% conversion, removal from heat block.

## Slide 10
Waste
Eluent
Eluent pump
Heat and stir plate
Polymer pump
Dialysis module
Purge
solvent
NMR
Overpressure release
Deuterated solvent
10 mL syringe pump
Gas manifold
Linear actu-ator
Module 2 – Dialysis module
Gas in: always port H
Purge solvent in: always port G
To reaction vial: always port A
To waste: always port E
Start dialysis pumps and counterflow polymer and eluent.
Monitor decaying vinyl signal in NMR (until again 90% of signal gone)
Pump polymer back to vial
Argon supply

## Slide 11
Waste
Eluent
Eluent pump
Heat and stir plate
Polymer pump
Dialysis module
Purge
solvent
Purge
solvent
Stock solutions
10 mL syringe pump
UV/VIS
Gas manifold
Linear actu-ator
Module 3 – Endgroup modification module
Gas in: always port H
Purge solvent in: always port G
To reaction vial: always port A
To waste: always port E
Deoxygenation by argon sparging (for 10 min)
Addition of aminolysis agent in DMSO (Octylamine + Na2S2O4 (as antioxidant))
Start stirring (reaction at room temperature)
Monitor decaying UV/Vis peak around 520 nm
After full decay, go back to module 2 and do dialysis for 4 hours
Argon supply

## Slide 12
Argon supply
Waste
Heat and stir plate
MeOH
Purge
solvent
Solenoid valve
Precipi-tation vessel
Gas manifold
Linear actu-ator
Module 4 – Precipitation module
Gas in: always port H
Purge solvent in: always port G
To reaction vial: always port A
To waste: always port E
Pump methanol (ca. 30 mL) into precipitation column (open corresponding side of solenoid valve)
Open other side of solenoid and apply argon flow from bottom through methanol
Aspirate and dispense polymer into methanol from top
Remove methanold by aspiration with syringe pump and dispose of it
Add more methanol (ca. 20 mL) and bubble argon through for 5 min
Aspirate methanol and dispose of it
Dry polymer on frit with argon flow from bottom
(Potentially aspirate DCM and dissolve polymer and put it into a vial elsewhere)
Clean the whole setup by purging everything with purge solvent